| Thermalsil™ III Thermally Conductive Silicone Rubber Insulators The newest Thermalsil™ III formula has improved thermal conductivity, providing excellent thermal resistance. It is used as an electrically-isolating interface material composed of silicone elastomer binder with a thermally conductive filler. It is reinforced with glass cloth to resist tearing and cut-through due to burrs on transistors or heat sinks. Thermalsil™ III eliminates the need for grease application and conforms to mounting surfaces under clamping pressure for optimum heat conduction. Thermalsil™ III is .152mm (.006") thick and grey green in color. A finely woven glass cloth provides the thinnest possible matrix for enhanced thermal resistance. To order Thermalsil™ III with adhesive coated backing, add suffix "AC" to the part number. For example, 53-03-2AC. Thermalsil™ III is available in any configuration with adhesive backing. Order by adding "AC" after the part number. For example: 53-03-2AC. |
| --- |
| Thermalsil™ III |  |
| Property Typical Value 25°C Test Method Electrical Dielectric Constant 2.5@50 Hz 2.5@103 Hz 2.5@106 Hz ASTM D150 Dielectric Breakdown Voltage 26.3 x 103 volts/mm (667 volts/mil) ASTM D-149 ASTM D149 Volume Resistivity 5.7 x 1015 ohm-cm ASTM D257 Dielectric Dissipation Factor .008@50 Hz .004 @103 Hz .004 @106 Hz ASTM D150 Physical Thickness .15 + .03/-.05mm (.006 + .001/-.002 in.) Color Gray-Green Tensile Strength 6.1 x 107 Pa (8786 psil) Hardness, Shore A 87 Elongation 2% or less Thermal Thermal Conductivity 0.92 w/m °C Flame Resistance UL 94V-0 UL card #E-58126 (S) Service Temperature -60°C to 180°C (-76°F to 356°F) |
| Standard Thermalsil Configurations |  |
| Part Number A B C D 53-78-1* 22.10 (.870) 1.57 (.620) |

* This insulator is made especially for clip-mount heat sinks, thus requiring no mounting hole.