	Insulating Shoulder Washers
RoHS Compliant 

· 40% glass filled polyphenylene sulfide (PPS). 

· Chemically inert [no known solvents under 200°C (392°F)] 

· Maximum recommended service temperature of 260°C (500°F) 

· Recommended torque is .565Nm to .678Nm (5 to 6 inch-pounds) on all shoulder washers except -7, which has recommended torque of .452Nm (4 inch-pounds). 
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Polyphenylene Sulfide PPS Shoulder Washers 

Note: A single gate extension, not to exceed .64mm (.025") in length, is allowable on the outside of all shoulder washers.
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* Also for M3 Screw
	


